TOWEL DYE

We package dye for ease of use in institutional laundries. These dyes come in safe and easy to dispense water soluble packages. These dye paks are great for color coding 100% cotton textile goods as well as blends. The dye is not a permanent dye but it is our most economical and easiest to use. If you need a more permanent dye try using Colourfast dye kits. All of our dyes are available in many colors and included is a shade card displaying our stock colors. Custom Color matching is available.

Maintenance, Power Pak  and Super Towel Dyes

Instructions For Dyeing Towels and 100% cotton*

New fabrics should be thoroughly cleaned at high temperatures using an alkaline detergent to remove sizing.

| Operation | Level | Temperature | Time | Supplies |
| --- | --- | --- | --- | --- |
| 1. Wash | Low | 175 Degrees | 10 to 15 | 1lb. Alkaline detergent per 100-lb load |
| 2. Rinse | High | Hot | 2 |  |
| 3. Dye | High | 150-180 Degrees | 15* | 2-3 packets dye per 100-lb load |

**The addition of salt at 4 lbs. per 100 lb of load will considerably increase the speed of dye exhaustion through the load.

Instructions For Touch-Up Dyeing

The dyeing operation should be the second hot rinse after the last detergent bath.

| Operation | Level | Temperature | Time | Supplies |
| --- | --- | --- | --- | --- |
| 1. Dye | High | 150-180 Degrees | 5-10 minutes | 1 packet dye per 100-lb load |

Rinse clear after dying.

Black         Blue          Navy          Royal        Brown       Green

Br. Grn      Orange      Red           Garnet        Violet        Yellow