#### HOTEL DYE PAK

This dye pak is designed to dye cotton fabrics to color. The Keyfix included in the pak extends color wash life. Each kit will dye a minimum of 500# of fabric.

DYEING PROCEDURES

STEPS  1.	Load clean  towels and  DYE ( 2 Paks / 100 lbs of load.) into washer

2.	Fill washer to high level with hot ( 150( to 170(F ) water. Run for 20 	minutes

3.	Drain

4.	Fill washer to high level with 120(F water. Add  8 oz.  KEYFIX / 100 lbs. of load. Run 10 minutes.

5.	Drain

- Follow with 4 to 6 high level, cold water rinses until drain water is clear.

- Washer can be rinsed with hot water and bleach to remove dye residue.

Hotel Dye Pak colors include: Navy, Red, Blue, Yellow, Orange, Brown, Royal, Black, Green, and Violet.

###### Dye Formula

Load washer with clean towels and dye

Suggested : 2 paks dye for each 100 lbs of load

| OPERATION | LEVEL | TEMP. | TIME MIN. | SUPPLIES |
| --- | --- | --- | --- | --- |
| 1 Dye / DRAIN | High | 150°/ 170° | 15-20 | 2 dyes paks per 100 lbs. load |
| 2 Fix / DRAIN | High | 120° | 10 | Add 1 bottle KEYFIX For each 100# of load |
| 3 Rinse / DRAIN | High | Cold | 2 |  |
| 4 Rinse / DRAIN | High | Cold | 2 |  |
| 5 Rinse / DRAIN | High | Cold | 2 |  |
| 6 Rinse / DRAIN | High | Cold | 2 |  |
| 7 Rinse til Clear |  |  |  |  |